## Slide 1: Analysis of the Cause and Effects of Part Defects in ABS Samples Made Using Additive Manufacturing Arshad Mohammed1, Boppana V. Chowdary2
1,2Faculty of Engineering, The University of the West Indies, Trinidad

## Slide 2
PRESENTATION OUTLINE
Introduction
Methodology
Results and Discussion
Conclusion
Future Research Agenda

## Slide 3
INTRODUCTION
Material Extrusion (MatEx) is an Additive Manufacturing (AM) technique of creating parts by depositing material through a nozzle
Top view of layer building process

## Slide 4
INTRODUCTION
Contour rasters
Infill rasters
Raster-raster airgap
Contour-raster interface
Contour-contour interface
Void between contours
Void between contour and raster
Raster angle
Road width
Top view and magnified of layer

## Slide 5
INTRODUCTION
Advantages of AM over traditional systems:
  High product customization possible
  Low cost and low lead time for small production runs
  Complex and functional
Challenges of AM:
  Many process parameters that directly affect the performance of the product
  The layer by layer process of AM also results in a reduction of strength of the part

## Slide 6
INTRODUCTION
Common trend in literature:
  Optimization of mechanical properties of parts made using MatEx
Focus of research:
  Investigate the failure of MatEx parts under compression
  Investigate the effect of annealing on MatEx parts

## Slide 7
METHODOLOGY
Design Test Specimen
Design Experimental plan
Build Specimens
Testing Specimens
Observation of failure
Classification

## Slide 8
METHODOLOGY
An IV-Optimal design of experiments was followed since it allowed for two categorical factors, in this case ‘infill type’ and ‘annealed’. A total of 18 experiments were run
Factor | Levels |  | 
 | Level 1 | Level 2 | Level 3
Layer thickness | 0.1 | 0.2 | 0.3
Road width | 0.3 | 0.35 | 0.4
Airgap | 0 | 0.025 | 0.05
Number of contours | 0 | 3 | 6
Build Orientation | 0 | 90 | 180
Infill Type | Lines | Honeycomb | -
Annealed | No | Yes | -
Table 1 summarizing factors and their respective levels

## Slide 9
METHODOLOGY
3D view of four layers
Honeycomb infill
Lines infill
Specimen being compressed

## Slide 10
Methodology
Samples were made using a Raise3d N2+
  Enclosed build chamber to maintain a consistent build environment
  Samples were built on the same day to minimize effect of varying external conditions
  After building they were stored in individual bags and an air tight container
All samples were tested on the same day, again to minimize external variations

## Slide 11
RESULTS AND DISCUSSION
Pareto Chart of process parameters and interactions

## Slide 12
RESULTS AND DISCUSSION
Various defects observed in the failed samples
Deformation
Layer Delamination
Raster Delamination
Contour-Infill delamination
Sheared layers

## Slide 13
RESULTS AND DISCUSSION
Cause and effect diagram of part failure under compression loading

## Slide 14
CONCLUSION
The failure for MatEx parts under compression were categorized into five forms, namely: Layer delamination, buckling, raster delamination, contour-infill delamination, shearing along layer
The most common form of failure observed was layer delamination
The top three influencers for compressive strength were annealing, the interaction of road width and layer thickness followed by layer thickness.

## Slide 15
FUTURE RESEARCH AGENDA
Optimization of annealing parameters
Investigation of failure under other loading conditions
Testing of recycled and composite materials
Quantitative analysis on the bond strength of rasters

## Slide 16
THANK YOU!